September 23, 2008

Testing was performed in accordance with:

ASCE 19-96, 3.2.2., which requires fittings to develop an ultimate strength of at least 110% of the specified nominal cable strength.

| Work Order No.: | 51828 | Lot No.: | 51828 | Date: | 11/1/06 |
| --- | --- | --- | --- | --- | --- |
| BRACE-GRIP® DE CAT NO. | STRAND SIZE (in.) | STRAND MBS (lbs.) | MAXIMUM LOAD (lbs.) | % MBS | FAILURE MODE AT MAX. LOAD |
| BRG-2586 | 9/16" EHS G.S. | 35,000 | 38,713 | 110.6 | All elements of strand failed midspan at max. load. No slip. |
|  |  |  | 38,732 | 110.7 | All elements of strand failed midspan at max. load. No slip. |
| AVERAGE |  |  | 38,722.5 | 110.65 |  |

Regards,

Scott L. Sanderson

Corporate Quality Assurance Engineer

ma

cc:  File 94

J. Reilly